## Slide 1: Updates
Olivier Bergeron

## Slide 2: Electrode Impedance Test
Electrode under test
Counter electrode
Saline solution 0.9%

## Slide 3: Electrode Impedance Test
Why this setup
  2 electrodes get closed electrochemical circuit
  Electrode impedance is defined by ionic transfer at electrode-electrolyte interface -> reason for ionic solution
  Why saline? Physiologically relevant
Keep environment the same from one electrode under test from another.
  Same distance between electrode under test and counter electrode
  Use same ionic solution

## Slide 4: Ricardo’s and Ankur electrodes

## Slide 5: Electrode Impedance Test
Issues with the patch
  Traces same material as the electrode: big impedance difference between one electrode to another
    40 mm longer traces between L1 – L2
  Cracks in the ink
  Connection issues

## Slide 6: Connection issues

## Slide 7: Intan read setup
Goal: Quick setup for reading EMG signals
What: RP2040
  Dual core MCU
    Core 1: SPI acquisition
    Core 2: USB streaming to PC

## Slide 8: Intan read setup
What has been done
  USB streaming works with dummy data
What to do next
  SPI data collection
  Saving data into PC

## Slide 9: Next steps
Prepare the impedance test setup
Continue EMG reading setup
Prepare post-processing algorithms (BSS, 2CFastICA, etc.)